## Slide 1: Superconducting nanowire single photon detectors and their performance in strong magnetic fields
December 10th, 2019
erhtjhtyhy
Tomas Polakovic
PHY Argonne
Drexel University
W.R. Armstrong, V. Yefremenko, J.E. Pearson, K. Hafidi, G. Karapetrov, Z.-E. Meziani, V. Novosad
CPAD 2019,
Madison, Wisconsin

## Slide 2: But why magnetic fields?
And other bad things…
Applications of quantum detectors outside of QIS
Nuclear/particle physics, cosmology, etc.

## Slide 3: But why magnetic fields?
Nature papers
Detectors

## Slide 4: Hostile conditions?
W. Armstrong
Detectors
Nature papers
And other bad things…
W. Armstrong

## Slide 5: But why magnetic fields?
Low energy recoil detector for photodisintegration of polarized deuteron targets
3He tagging in J-Ψ electron production
And other bad things…

## Slide 6: What do we need?
Fast + precise (>= 1GHz + ~10 ps jitter)
Rad hard
Mag field resistant (~3 T)
Not too cold (> 4.2 K)
Small

## Slide 7: single photon superconducting nanowire detectors
Devices utilizing superconducting nanowires biased close to critical currents
Excitation of quasi-electrons from a Cooper pair starts an avalanche process that turns the whole wire cross section normal
Transition is from a superconducting to fully normal, high resistance (>1 MΩ) state
  No squid current preamplification needed
Currently the best timing and rate photo-detectors available
Can also do particles not really an explored field
  Lack of interest (historically)

## Slide 8: Niobium Nitride as detector material
Technological complications
Rad hard?
  Yes. NbN is a crappy form of Zircalloy
Not too cold?
  Yes (TC > 8 K)
Can handle strong fields?
  Yes, Hc2(0) ~ 30 T
SC δ-cubic NbN
Non-SC δ’-hexagonal NbN
Thermodynamically stable

## Slide 9: Niobium Nitride as detector material
Technological complications
Rad hard?
  Yes. NbN is a crappy form of Zircalloy
Not too cold?
  Yes (TC > 8 K)
Can handle strong fields?
  Yes, Hc2(0) ~ 30 T
    Wait…What?
SC δ-cubic NbN
Non-SC δ’-hexagonal NbN
Thermodynamically stable

## Slide 10: How?
G. Berdiyorov, et. al., PRB (2014)

## Slide 11: How?
A.E. Koshelev, et. al., PRB (2016)

## Slide 12: Ion Beam Assisted Sputtering
Technology developed as a solution
Sputtering technique developed during NbN nanowire R&D
Replaces passive N2 gas with N plasma
Increased in particle energy eliminates need for high temperatures
Different momentum distributions allow for growth on non-epitaxial substrates
Invention report ANL-IN-17-164
Polakovic, et. al., APL Mat (2018)
Nb
Si
N2
Si
Nb
N+
e-
Conventional sputtering
IBAS

## Slide 13: Ion beam assisted sputtering of NbN
material properties
Growth of films achieved with bulk Tc as high as 14.5 K
ρN = 110 μΩ.cm – disordered films
Perpendicular Hc2 = 32 T (in-plane ξ=3.2 nm)
Reduced sensitivity to Nitrogen concentration
Textured (111) growth on Si substrates
No presence of non-superconducting phases of NbN
Process works at room temperature and on Si substrates
Polakovic, et. al., APL Materials (2018)

## Slide 14: Ion beam assisted sputtering of NbN
b = 0.73 Å
c = 2.84 Å2
τ = 2.43e-15 s
Devices typically use ultra-thin films
  Behavior of superconductivity in 2D limit has been explored
A superconductor-insulator transition is observed at thickness of approx. 2 nm
Can be explained either by electron wave leakage (quantization of order parameter) or weak localization (strong Coulomb interaction of electrons)
Both theories predict similar behavior
  Impossible to determine which effect is dominant
Polakovic, et. al., APL Materials (2018)

## Slide 15: Superconducting nanowire detectors
SC Nanowires at Argonne
Detectors capable of single-photon detection with saturated QE in fields up to 8 T
Operational temperatures of 4 K
Detection rates at least 100 MHz with 0 dark counts
Polakovic, et. al., arXiv:1907.13059 (2019)

## Slide 16: Superconducting nanowire detectors
SC Nanowires at Argonne
Detectors capable of single-photon detection with saturated QE in fields up to 8 T
Operational temperatures of 4 K
Detection rates at least 100 MHz with 0 dark counts
Polakovic, et. al., arXiv:1907.13059 (2019)

## Slide 17: Superconducting nanowire detectors
SC Nanowires at Argonne
Detectors capable of single-photon detection with saturated QE in fields up to 8 T
Operational temperatures of 4 K
Detection rates at least 100 MHz with 0 dark counts
Polakovic, et. al., arXiv:1907.13059 (2019)

## Slide 18: Superconducting nanowire detectors
SC Nanowires at Argonne
Detectors capable of single-photon detection with saturated QE in fields up to 8 T
Operational temperatures of 4 K
Detection rates at least 100 MHz with 0 dark counts
Current characterization focus on high-energy photons
Particles + calorimetry soon
400 nm
900 nm
Polakovic, et. al., arXiv:1907.13059 (2019)

## Slide 19: Summary
We can fabricate SNSPDs with all their benefits that work in fields as high as 8 T
Preliminary results show no degradation in radiation fields of accelerators (ANL ATLAS)
Can operate at LHe temperatures (no need for additional expensive cooling facilities)
Stay tuned for particle ID and calorimetry in near future

## Slide 20
Thank you for your attention