## Slide 1: Development of a 3D detector on a hydrogenated amorphous silicon substrate
M. Menichelli(a), M.Boscardin(b)(c), M. Crivellari (c), J.Davis(f), S.Dunand(i) , L. Fanò(a)(d), A.Morozzi(a)(g), F.Moscatelli(a)(e), M. Movileanu-Ionica(a), D.Passeri(a)(g) , M.Petasecca(f), M.Piccini(a), A.Rossi(a)(d), A.Scorzoni(a)(g), G.Verzellesi(b)(h), N.Wyrsch(i).
(a) INFN, Sez. di Perugia, Perugia (ITALY)
(b) INFN TIPFA, Trento (ITALY)
(c)Fondazione Bruno Kessler, Trento (ITALY)
(d) Dip. Di Fisica dell’Università degli studi di Perugia, Perugia (ITALY)
(e) CNR-IOM Perugia (ITALY)
(f)Centre for Medical Radiation Physics, University of Wollongong, NSW 2522, (AUSTRALIA)
(g)Dip. Di Ingegneria dell’Università degli studi di Perugia, Perugia (ITALY)
(h) Università di Modena e Reggio Emilia, Modena (ITALY)
(i) Ecole Polytechnique Federale de Lausanne (EPFL), Institute of Microengineering (IMT), Neuchatel, (SWITZERLAND)

## Slide 2: Hydrogenated Amorphous Silicon a-Si:H
The first study on a-Si:H was reported by Chittik et al. in 1969
Material was obtained by plasma-enhanced chemical vapor deposition (PECVD) of SiH4 (Silane) + Hydrogen.
Substantial progress of the a-Si:H technology were performed when Spear and Lecomber demonstrated that this material could be substitutionally doped (both in n and p-types); this led to the development of various types of electronic devices such as transistors, solar cells, memories and eventually, in the second half of the 80’, planar radiation detector in p-i-n structures.

## Slide 3: A-Si:H Structure and density of states

## Slide 4: A-Si:H planar detectors pros & cons I
Pros:
  Extremely low radiation damage.
  Low cost production (this technology is currently used in solar cells production)
  Possible deposition in many different substrate materials

## Slide 5: A-Si:H planar detectors pros & cons II
Cons
  High depletion voltage (about 1100 V for 50 um thickness)
  Growth on a non-removable substrate
  Pretty low charge collection efficiency: 50%(on a 30 um thick detector) energy to create a e-h pair similar to crystalline silicon (3.4-4.0 eV)
  High leakage current (in the order of few uA/cm2 on a 30 um detector)
  Low mobility (from 1 to 10 cm2 /Vs for electrons 2 orders of magnitude less for holes)
  Limited thickness of substrates (max 100-150 um)

## Slide 6: Displacement damage on a 30 um a-Si:H planar detector

## Slide 7: Signal formation on planar a-Si:H detectors

## Slide 8: 3D technology on a-Si:H
The depletion potential applies on the interelectrode distance that is not coincident with the thickness of the detector
Never attempted before
Noise reduction test at cold temperature (e.g. -30°C)

## Slide 9: Baseline 3D detector structure

## Slide 10: Possible 3D detector configurations

## Slide 11: Technological options for doping the electrodes
Option 1: Selective layers of metal oxide deposited via ALD
Option 2: Ion implantation and low temperature activation (250 °C or below )

## Slide 12: Prototype development
Phase 1: construction of planar diodes with option 1 and 2 doping techniques.
Phase 2: Construction of basic 3D structures in order to test the two proposed doping techniques.
Phase 3: Construction of 3D detectors in various configurations.

## Slide 13: Diodes and test structures layout in phase 1 prototypes
Before depositing a-Si:H the p-type silicon wafer is divided in two halves and in one of the two halves is oxidated.
In the non-oxidated half vertical diodes are fabricated
In oxidated half lateral diodes are fabricated

## Slide 14: Vertical diodes

## Slide 15: Lateral diodes

## Slide 16: Final complete Layout

## Slide 17: A-Si:H material simulation
Parameter (units) | Literature | Simulation
Relative permittivity | 11.8-11.9 | 11.7
Electron mobility (cm2 V−1 s−1) | 0.5-20 | 10
Hole mobility (cm2 V−1 s−1) | 0.003-10 | 0.01
Band Gap (eV) | 1.7-1.9 | 1.84
Dangling bond density (cm-3) | 5 x 1014 – 5 x 1016 | 4 x 1015
Activation energy (eV) | 0.42-0.49 | 0.52

## Slide 18: Defects model

## Slide 23: Timeline of the 3 years program
Tape out of the phase 1 prototype. DONE
Completion of production of the phase 1 prototype by January at most.
Testing of the phase 1 prototype and beginning of definition of the phase 2 prototype by april 2020
Construction of phase 2 prototype by mid 2020.
Testing of phase 2 prototype and design of the phase 3 prototype by the end of 2020
Production and testing of the phase 3 prototype by the end of 2021

## Slide 24: The future of 3D a-Si:H detector
Fabrication of an actual pixel detector bump-bonded on a readout chip.
Deposition of a-Si:H directly on the readout chip and construction of the 3D detector on the deposited substrate.