## Slide 1: Probing the Neutrino Mass with PTOLEMY
Andi Tan
Princeton University
CIPANP 2025 @ UW–Madison
June 11, 2025
Princeton
Tritium
Observatory for
Light,
Early-universe,
Massive-neutrino
Yield

## Slide 2
??
0
Super-Kamiokande
Sudbury Neutrino Observatory (SNO)
Neutrinos are produced or detected in flavor eigenstates but propagate in mass eigenstates which causes the oscillation.
Oscillation gives the and . Therefore, 2 possible mass hierarchies exist.
The absolute mass of the lightest mass eigenstates is unknown.
Notes: The absolute mass of the lightest one remains unknown.
We will hear from our upcoming speaker about how they can gain their mass theoretically.
And I will focus on the experimental progress on the direct mass measurement.

## Slide 3
Observable
0.028-0.122 eV from KamLAND-Zen
Depend on Majorana nature and nuclear matrix element
arXiv:1006.0689
arXiv:2504.20038
arXiv:2203.02139
Observable < 0.062 eV Depend on ΛCDM
Kinematic determination of neutrino mass is a direct, model-independent method.
Notes: Cosmological constrain on the sum of their masses depend on the analysis framework, or Standard Model of cosmology, the ΛCDM model.
0vbb constrain depends on the Majorana nature and nuclear matrix element calculations.
These methods access the neutrino mass scale indirectly.
A direct, model-independent method is needed to determine the neutrino mass.
And we must use just kinematics.
Snomass: https://arxiv.org/pdf/2209.03340.pdf
Simulation: https://physics.aps.org/articles/v3/57

## Slide 4: Cosmic Neutrino Background
Frozen-out at s
Temperature
Number Density
per flavor
Momentum/Velocity Distribution
For meV,
Dicke, Peebles, Roll, and Wilkinson, 1965,
“Cosmic Black-Body Radiation.,” Astrophysical J 142, 414.
Notes: On the other hand, neutrinos are not just the portal to new physics from particle physics.
It played an important to role in the early Universe and throughout its evolution.
This is a 1965 paper by Bob Dicke, Jim Peebles, Peter Roll and David Wilkinson called the “Cosmic Black-Body Radiation”.
This is a back-to-back paper with the Penzias & Wilson which discovered the CMB.
In this paper, they proposed the thermal history of the Universe which condensed in this plot with three curves.
We have the radius of the Universe on the bottom and the corresponding time (its age) on the top.
Two curves of matter and radiation density with their axes on the right and the temperature curve with its axis on the right.
Follow the milestones below and tracing back in the history of the Universe, the first dash line indicates the recombination of the plasma and the produce of the CMB, before that, the matter and radiation are in equilibrium.
The 2nd dash line shows the matter-radiation equality where the Universe transitioned from a radiation-dominated to a matter-dominated one.
We are interested in the even early milestone here it says, “opaque to Neutrinos”.
At about 1 sec, the neutrino fireball decoupled from the rest of the Universe and propagate and expend independently.
If you look at the kink in the temperature curve, short after the neutrino freeze-out, the detailed balance between electron-positron pair production-annihilation breaks.
Therefore, their entropy transferred to the photons which slows down the cooling of the photons.
Through this connection and based on the precise measurement of the CMB, we know that the temperature is about 1.95K (kT~0.168 meV);
The number density is 112/cm3 per flavor.
Momentum is still F-D wih T~0.168 meV so the average velocity is inversely proportional to the mass.
For mass 50meV, v/c is 1.4 percent and thus they are nonrelativistic.

## Slide 5: In Fermi’s 1933 seminal paper (English Trans.)
Notes: Back to Fermi’s 1933 seminal paper, he had already shown how one can do this.
This is an English translation. In Fig.1, he showed that the end point of the electron spectrum bears the information of the neutrino mass.
In his notation, E0 is not Q value but the max energy of beta ray and mu is the neutrino mass, not its magnetic moment.

## Slide 6: and CNB with Tritium
* Weinberg,. Phys Rev 128, 1457–1473 (1962). **Cocco, Mangano & Messina, J Phys Conf Ser 110, 082014 (2008).
n
p
p
n
p
n
n
p
p
n
p
n
Steven Weinberg laid out basic concepts for CNB detection in 1962
Cocco, Mangano, Messina applied to massive neutrinos in 2007
Tritium as target:
High ,
Availability,
Lifetime,
Low .
Notes: Basic concepts for relic neutrino detection were laid out in a paper by Steven Weinberg in 1962 and applied for the first time to massive neutrinos in 2007 by Cocco, Mangano, and Messina.
If you have a beta emitter, say tritium, it decays into helium and emits an electron and an anti-electron-neutrino.
Now, we apply crossing symmetry to this reaction. These beta nuclei can act as targets for capturing incoming electron neutrinos.
In this case, it becomes a two-body decay.
The electron emitted will have higher energy than those electrons from the reaction on the left.
It turns out that tritium is the most promising target candidate because of its
availability, lifetime, high neutrino capture cross-section, and low Q-value.
There are many recent studies about the capture target, and I will come back to this later.

## Slide 7: and CNB with Tritium
JCAP 2019, 047–047 (2019).
Increase S/N ratio by
filtering away the low energy electrons to the last 1eV window, which increases by ;
cutting-edge energy resolution , i.e., .
Notes: So, this is sort of a rare event search experiment.
S/N ratio becomes the figure of merit.
We hope to increase the sensitivity by
1. Filter away the low energy ones to the last 1eV window
increase by 13 orders of magnitude from to ;
2. After those electrons slow done to sub eV level, measure their energy precisely.
increase 𝜆_𝜈∕𝜆_𝛽 by 13 orders of magnitude from 0.66×10^(−23) to 3.×10^(−11);

## Slide 8
Micro-calorimetry
Decay products dump energies to heat up the absorber.
Measure ΔT.
Electromagnetic spectrometry
Trap electrons in B field and adjust electric potential hill to filter.
Cut-and-count
Cyclotron Frequency Spectroscopy
Accelerating electrons radiate photon – cyclotron emission
Measure frequency.
Credit: Jörg Enderlein
Notes: I will review three methods in this field.
On the left, one can do it with an electromagnetic field where we trap the electrons in the B field and push them up to an electric potential hill.
Only those electrons with high enough kinetic energy can reach the other side of the hill.
By adjusting this hill, we can perform a cut-and-count measurement.
In the middle, recent developments on the frequency-based technique had emerged in this field.
By measuring the faint radio-frequency emitted from gyrating electrons precisely, one can extract its kinetic energy.
On the right, micro-calorimeters has been used to measure the de-excitation spectrum of the Dysprosium-163.
The cascade decay products dump their energies to heat up the absorber and cryogenic thermometers are used to measure the temperature rise.

## Slide 9
Micro-calorimetry
Measure ΔT
Energy resolution eV
Sensitivity Goal: 1 eV
Electromagnetic spectrometry
Cut-and-count
Energy resolution eV
Sensitivity Goal: 0.2 eV
Cyclotron Frequency Spectroscopy
Measure frequency
Energy resolution eV
Sensitivity Goal: 40 meV with atomic source.
E
C
G
t=
C

## Slide 10
HV
18.6kV
Target:
Relic Neutrino
Capture
RF Tracker:
Electron Pre-Measurement
Dynamic Filter:
Selects endpoint electron in narrow 10-4 energy window
Micro-calorimeter:
Measures few eV electron to 10-2 energy resolution
Notes: The block diagram of our experiment is the following.
We first have a target surface that holds beta-decaying nuclei which relic neutrino capture.
We then have a tracking system. It assesses whether the electrons are near the endpoint of the spectrum we are measuring and the pitch angle.
The angle between the electron momentum and the direction of the magnetic field.
With that dynamic information, we can transfer the electron through a slow drift process from the target to the filter region.
We configure a precision electromagnetic filter that is extremely compact.
The electrons go through bouncing and cyclotron motions in the filter.
It pushes the electrons from 18.6 keV endpoint energy up an electric potential so the electrons finally have down to a few eV which can be measured by a calorimeter.
We use micro-calorimeter transition-edge-sensors (TES) with a dynamic range of a few eV to measure the kinetic energy to achieve 10E-2 eV energy resolution.

## Slide 11
atomic H as a tool to ‘pinch’ the sp2 bonds towards a sp3 configuration while maintaining the planar nature of graphene
sp3 C-H bond
Hydrogen and Deuterium loading on graphene at Roma1 and Roma3
Betti et all, Nano Lett. 22, 2971 (2022)
UKAEA’s Active Gas Handling System (tritium for JET, EU Tokamak) for feasibility study & design requirement of a new T loading chamber
Quote received
H on Nanoporous Graphene (NPG):
T-chamber in Rome side view:
Notes: 11

## Slide 12: Solid State Effects on Tritiated Graphene
Various final states of induce features in the electron spectrum
To determine the final helium binding potential is very subtle
arXiv: 2504.13259v1
12

## Slide 13: Solid State Effects on Tritiated Graphene
Different ways of implementing the sudden approximation led to different predicted rates
The paper studies this and other solid-state effects. It also provides a first rough rule of thumb to determine the theory systematics on
arXiv: 2504.13259v1
13

## Slide 14: EXB Drift in the RF Region
We design a demonstrator with an electromagnet, a vacuum system, and an electric field cage.
A C-type magnet with iron extensions is built to produce field with
a strong, uniform field between poles,
an exponential decay field along +z,
constant curvature.
Notes: This is our design of a demonstrator to produce the B and E fields we want.
The idea is to use the fringe field of an existing C-type dipole magnet.
We used a trick to attach iron extensions to the main return yoke.
The extensions “steal” some flux from the main yoke and short-circuited it to the poles.
These fluxes then create a magnetic pressure that pinches the fringe field.
With a longer extension, some flux actually just hops over the air from one arm and enters the other arm.
Which creates a quadrupole point with a zero B field where we can place our calorimeters.
In this way, we can have an exponentially decaying Bx field with constant curvature.
We also design a vacuum system and an electric field cage with it.
We design a demonstrator with an electromagnet, a vacuum system, and an electric field cage.
A C-type magnet with iron extensions is built to produce 𝐵_𝑥 field with
a strong, uniform field between poles,
an exponential decay 𝐵_𝑥 field along +z,
constant curvature.

## Slide 15: EXB Drift in the RF Region
With a C-14 source, we have demonstrated the control of the EXB drift velocity (slowing by X5)* by manipulating the voltage on electrodes.
*limited by the size of the electrode in this demonstrator
arXiv 2503.10025

## Slide 16: EXB Drift in the RF Region
The event rates agree with simulation by changing the drift speed.
We can also measure the 1D activity profile of the source disk by shifting the y acceptance region.
*limited by the size of the electrode in this demonstrator
arXiv 2503.10025

## Slide 17
RF detection setup at LNGS: electron trap
17

## Slide 18
Candidate electron events
RF emission frequency vs time of single electron in the permanent magnet
Carrier
Secondary
P[W]

## Slide 19
Candidate electron events
RF emission frequency vs time of single electron in the permanent magnet
Carrier
Secondary
Source: 85Rb → 83mKr Life time Kr = 158.1 min

## Slide 20: Electromagnetic Filters
KATRIN
~1200m3
mn < 0.8 eV/c2 (90% CL)
Nature Physics 18,160–166 (2022)
arxiv 2105.08533
0.2 eV/c2 Sensitivity Goal
(~1 eV energy resolution)
Magnetic Adiabatic Invariance
Collimation: -𝛻B||B
Reflect for E<Efilter
Pass for E>Efilter
Notes: The state-of-art experiment of beta spectrum endpoint measurement is the KATRIN experiment.
They use an electromagnetic filter based on the conservation of magnetic adiabatic invariances called the MAC-E filter.
The basic idea is to first create a magnetic “mirror” machine, or a magnetic bottle, as in Jackson’s textbook.
The schematic on the left show half of the geometry with a strong magnetic field on the bottom left, typically created by coils.
The magnetic field lines splay out to a vast region and thus the B field decrease which has a gradient parallel to the B.
Then, if you apply an electric field along the B field, it becomes a filter.
It aligns the momentum of the electrons and collimates them.
Those with kinetic energy less than the filter threshold will bounce back and forth in the bottle
And those with excessive kinetic energies can pass.
So, it’s a high-pass energy filter, and then you can perform a cut-and-count measurement.
On the right picture is their famous 5-story high main filter with a sheer volume of about 1200 cubic meters.
Their current result is 0.8 eV/c2 90% C.L., and with more statistics, they may reach their goal of 0.2 eV/c2.
However, this filter can only reach about 1eV energy resolution.

## Slide 21: Electromagnetic Filters
PTOLEMY
~1m3
Magnetic Adiabatic Invariance
No Collimation: -𝛻B⟂B
Transverse Drift filter
Notes: We propose a new type of filter, a much COMPACT one, dubbed transverse drift filter.
We also exploit the adiabatic invariance by looking for a magnetic gradient.
Instead of having a gradient parallel to the B field, we look for a gradient perpendicular to the B field.
We can use the fringe field between a pair of separated coils with a much faster decaying B field.
But this introduces the 𝛻B drift.
Then we create an E field, to balance the 𝛻B drift and also push the electron climbing a potential hill and loss its kinetic energy.
This is a magnet I built to generate a B field with the traits we need.
And its active volume is only about 1 cubic meter.
This allows scalability for our future experiment design.

## Slide 22: Full Demonstrator Simulation

## Slide 23
Filter Acceptance
Showing θ = 20±5, 30±5, 40±5 degrees averaged over Φ bins

## Slide 24
Based on the expertise of the INRiM electron detection with TES! Key elements: high quality TES and new e-source based on nanostructures
Phys.Rev.Applied 22 (2024) 4, L041007
Measuring Low-energy Electrons with TES
24
Full absorption peak @ 101 eV with a sigma of 0.3 eV
Characterization
ADR cryostat

## Slide 25: PTOLEMY first physics goal: neutrino mass
We plan to reach neutrino mass sensitivity of below 150 meV in 5 years
  Exploiting a novel concept of a compact dynamic electromagnetic filter
  Using O(10 mg) of atomic T to measure the tritium spectrum endpoint
25

## Slide 26
PTOLEMY Demonstrator
aims at showing the capability of the PTOLEMY collaboration to master technologies
Integration of all sub-components to achieve full electron transport
Spectrum measurement of tritium electrons
Measurement with O(eV) resolution
New option for first e-measurement in low magnetic field
are under investigation: modified Skipper/CCD
Final mass sensitivity goal by using about 10 mg of tritium
on graphene
26

## Slide 27: Sensitivity as a function of tritium mass
Remarks:
- the sensitivity is weakly dependent upon the energy resolution (500 meV is already a good starting point)
1 μg (7x7 cm2) already provides competitive sensitivity
- 100 μg (0.5 m2) can potentially probe the neutrino mass down to the IO scenario
(No systematic uncertainty included)
27

## Slide 28: To conclude:
Graphene hydrogenation demonstrated, to be implemented with tritium loading
Conductive-cooling MgB2 Superconducting Magnet ready at LNGS by the end of 2025, electrodes design ongoing
RF radiation detection well advanced - to be integrated in the demonstrator
Several electron source for calibration, HV stability approaches requirements.
First detection of 100 eV electron with TES, under consideration a warm detector based on electrostatic analyser commercially available with 50 meV resolution
Aim for reaching neutrino mass sensitivity of below 150 meV in 5 years
28

## Slide 29
Demonstrator parts under constructions: magnet, order issued
Magnet: Key subsystem
ASG (Genova)/Suprasys(Bilbao)
29

## Slide 30
HV filter electrodes feedthrough
Vacuum
station
Antenna signal FT
top or bottom or both
Cold source
For vacuum
environment
Volume hosting G-T sample
with standard CF flanges with
possibility to make it longer and
connected to vacuum suitcase
for G-T transfer. Possible adapter to be added afterword
Vacuum gauge
Vacuum gauge
(not visible)
Cylindrical volume hosting future electron detector
(not drawn)
120 cm OD
200 mm OD
ALCA technology (Vicenza)
order issued
Demonstrator parts under constructions: vacuum chamber

## Slide 31: Cosmic Neutrino Background
Hydrogen
Chlorine
Gallium
Deuterium + Cherenkov
The CNB is shown for a minimal mass spectrum here for 0, 8.6, and 50 meV, producing a blackbody spectrum plus two monochromatic lines for nonrelativistic neutrinos with energies corresponding to their masses.
Detection requires a reaction with no threshold.
Produce from RMP 92, 045006.
Notes: But we are on the most left part of the spectrum.
The two lines are the spectrum of reference masses of 8.6 meV and 50 meV.
We need some novel techniques to detect those low-energy neutrinos.

## Slide 32: PTOLEMY Electromagnetic Filter
Control electrons by:
field
Bounce potential
Filter (push them up the potential hill) & Guide them to the colorimeter by:
drift
drift
Curvature
term drifts along the equal potential lines. Therefore, combine it with term.
Side
View
Notes: But the electrons emitted in every direction, we need to use B and E to confine them and guide them to the calorimeter.
By applying a B field and a bouncing potential, the electrons with different pitch angles will be trapped in the EM field and move in harmonic oscillation, helical oscillation and a circle;

## Slide 33: mCal - Transition-Edge Sensors
Thin sensors: ~1 eV electron can be stopped few nanometer absorber with very small C
E
C
G
t =
C
Mauro Rajteri, Eugenio Monticone and others, https://doi.org/10.1007/s10909-019-02271-x
“TES Microcalorimeter for PTOLEMY”, J. Low Temp. Phys. 199 (2020) 138-142.
Notes: Transition-edge-sensors are thin film metals that were configured in the transition edge between its superconducting phase and normal phase.
This is a plot showing the resistance of a TES. You can see a very sharp transition between the two states.
When the incident electron dumps its energy in the thin film with a small heat capacity, it produces a huge temperature pulse as indicated on the top right.
The fast response time is achieved by design with large thermal conductance between the film and the bath refrigerator.
The temperature change causes the resistance change. Then it will be connected with an inductor coupled with a SQUID which enables the read-out.
TES for UV/NIR is a good candidate for detecting also electrons
Thin sensors: ~1 eV electron can be stopped few nanometer absorbers with very small C
Fast response time (t <1 usec)
Optimize TES for low-energy electrons with an energy resolution,
Goal: @
TESs for UV/NIR good candidate to detect also electrons
Thin sensors: ~1 eV electron can be stopped few nanometer absorber with very small C
Fast response time (t <1 usec)
Optimize TES for low energy electron with an energy resolution
∆=2.35√(〖4𝑘𝑇_0^2 𝐶〗∕𝛼 √(𝑛∕2)) ∝𝐸^□(64&1∕3)
Goal: ∆~50(22) meV @ 10(0.8) eV

## Slide 34: TES development
TES evaluated initially by IR photons in ADR setup at INRiM
ADR
setup
Optical fiber
TES SQUID
TES Layout 2021
Thermal bath
Si
Nb
wiring
Ti 12 nm
TES
Au 30 nm
SiNX 500 nm
SiNX 500 nm
20x20 µm
100x100 µm
10x10 µm
50x50 µm
Optimize the thickness of Ti/Au to tune energy resolution , where t is Ti Thickness.
Supported by
Notes: In our design, a 30 nm gold layer on the top will act as absorber to stop the incoming electron.
It has a very small heat capacity. A Ti layer goes superconducting.
This was done at INRIM institute at Torino, Italy.
This is one chip with four TES sensors.
We are optimizing the thickness of Ti/Au layer to tune the critical temperature and energy resolution.
The TES are evaluated initially by Infer-red photons in an ADR setup.
JTF

## Slide 35
Resolution of ~ mn :
Area ~ 15 mm x 15 mm
 Demonstrate with electrons
Area (µm2)
ΔE (meV)
DFWHM = 0.114 eV
Area = 400 mm2
Tc = 40 mK
EIR = 0.8 eV
DFWHM = 0.114 eV
Notes: This is an IR counting spectrum of one TES fabricated last month.
1540nm photons were used with 0.8eV.
We achieved 0.114 eV resolution for this device.
From this spectrum, you can see this device already has a dynamic rage of about 10 eV.
If we take this thickness parameter and scale its resolution with its dimension.
The optimal area for our required resolution at 50meV will be 15 by 15 um.
We are fabricating devices to demonstrate this resolution with IR and then demonstrate with electrons.
So, this is a very exciting step for us to keep pushing and have this ultra-precise calorimeter for the energy measure.
Now, we need to really understand whether we can transport the electron to the calorimeter.

## Slide 36
Alternative Energy Measurement
Electorstatic analyser
PTOLEMY e.m. filter exit
Ep
Ep- dE
Ep + dE
MCP
Anode
Delay Line
Helmholtz – Lagrange law
preamp.
CFD
TDC
Position sensitive detector (MCP+delay line)
allows parallel acquisition
Electrostatic lenses
Electron optic basic equation
Energy resolution
(bandpass energy):
DE: energy resolution
Ep : pass energy
x: slit width
R0: mean radius
q: accepted angle
Two concentric hemispheres
for the energy selection
Specs Phoibos 225

## Slide 37: PTOLEMY World-Wide Collaboration
Telescopio di neutrini cosmologici
Cosmic neutrino telescope
Telescopio de neutrinos cósmicos
טלסקופ ניטרינים קוסמיים
Kosmische neutrinotelescoop
Kosmisk neutrinoteleskop
2015 Targeted Grant Award from the
Chris Tully
Wonyong Chung
Mark Farino
Yunona Iwasaki
Notes: PTOLEMY is a worldwide collaboration with ~50 scientists from various institutes across the States,
many collaborators from Netherlands, Italy, and other countries as well.
At Princeton, I work closely with our PI, Prof. Tully, grad student Wonyong Chung, Mark Farino, and undergrad student Yuno Iwasaki.

## Slide 38: Papers in preparation
Transmission of electrons through graphene layers
Measurement of stability of tritium on graphene holder
The beta-decay spectrum of Tritiated graphene: combining nuclear
and Quantum mechanics with Density Functional Theory
General voltage stability system for full energy scale
Further improvement on electron detection with TES
Submitted
A Demonstration of Slowed Electron E×B Drift for PTOLEMY (arXiv:2503.10025)